ILLINOIS TOLLWAY									AC-160

CHECKLIST FOR
PORTLAND CEMENT CONCRETE PAVEMENT

This checklist has been prepared to provide the field inspector a summary of easy-to-read step-by-step requirements relative to the proper construction of PCC Pavement (Section 420).  The following questions are based on information found in IDOT Standard Specifications, IDOT Highway Standards, IDOT Constructions Manual and current policy memorandums and letters and Tollway Supplemental Specifications.

Have you checked the contract Special Provisions, Supplemental Specifications and plans to see if any modifications have been made to the requirements listed herein?	____

# 1.	DRAINAGE

Is the subgrade being kept drained during all operations?  Are all berms of earth deposited adjacent to the grade being kept drained by cutting lateral ditches through the berms? (Article 301.09)	____

2.	SUBGRADE AGGREGATE

Has the Subgrade Aggregate Source been approved?

If existing Concrete is to be recycled as the PGE component of the Subgrade Aggregate, does it meet the following requirements:		____

- Has the concrete removal method been approved by the Engineer?		____

- Are the bituminous and concrete materials being removed and separated as specified without contamination of dirt and foreign matter?		____

- Are stockpiling pads being provided at the crushing location?		____

- Do the PGE aggregate gradations comply with the specifications for the proposed material source?		____

- Does the PGE aggregate contain steel slag or any material that is considered expansive by the Tollway? 		____

Is the PGE component of the Subgrade Aggregate being placed and compacted uniform in gradation?		____

If reclaimed asphalt pavement (RAP) of the shoulders or overlays is to be recycled as the capping stone component of the subgrade aggregate, does it meet the following requirements:

- Is 100% of the processed RAP passing the 3 inch (75 mm) sieve?		____

- Is the processed RAP well graded down through the fines?		____

- Do all portions of the RAP capping stone contain less than 10% steel slag?		____

Has each lift of the Subgrade Aggregate been compacted to obtain the desired keying or interlock and necessary compaction?		____

# 3.	SUBGRADE/SUBBASE TRIMMING

Has the subgrade and/or subbase been trimmed prior to paving? 
(Article 420.04)	____

When forms are used to pave, is the trimming being done with a subgrade planer (Article 1103.08) or subgrade machine (Article 1103.09) prior to paving? (Articles 420.04 & 301.07)	____

When a slipform paver is used, is the trimming being done with a subgrade machine (Article 1103.09) prior to paving? (Articles 420.04 & 301.07)	____

# 4.	SUBBASE THICKNESS TEST

After trimming, is the thickness of the subbase being checked by any method at every 250 ft location or less?	____

Are all these job control thickness tests being recorded and retained as part of the job records? (Articles 311.07 or 312.31)	____

If locations of subbase have a deficient thickness, are they being corrected according to Articles 311.07 or 312.31 for the type of construction involved?	____

# 5.	PAVING FORMS

If paving forms are used do they meet the following requirements:

Are the forms: metal, not less than 10 feet in length, equipped with both pin locks and joint locks. (Article 1103.05)

Are the forms straight according to the following? (Article 1103.05)	____

- The form shall not deviate more than 1/16 inch from a straight line along the length of its upper edge.

- The longitudinal axis of the upstanding leg of the form shall not deviate from a straight line more than 1/4 inch in 10 ft of length along the length of its front face.

Is the height of form face not less than edge thickness of proposed pavement, the base width equal to or greater than the height, and are steel pins being used to secure each section? (Articles 1103.05 & 420.06)	____

Are the forms being set on a hard and true grade, built up in 1/2 inch maximum lifts of granular material in low areas (without using wooden shims) set not less than required for at least one days paving in front of the paver, and cleaned and oiled prior to the placing of concrete? (Article 420.06)	____

When wooden forms are allowed, are they full depth, smooth, free of warp, not less than 2 inches thick when used on tangent, and securely fastened to line and grade? (Article 1103.05)	____

Are curved forms of metal or wood being used on curves of 100 foot radius or less? (Article 1103.05)	____

Note:	Forms shall stay in place a minimum of 12 hours after concrete placement.

# 6.	FORM ALIGNMENT

Are you the Contractor checking the forms for line and grade and making necessary adjustments prior to concrete placement? (Article 420.06)	____

# 7.	LONGITUDINAL CONSTRUCTION JOINT

Are you marking the beginning and ending stations where adjacent curb, median, or pavement will necessitate the placement of deformed steel tie bars in the edge of the proposed pavement?	____

# 8.	SUPERELEVATION STAKING

Are you examining the plan curve data for all curves to determine where to stake the beginning and ending stations for all superelevation transitions?	____

By knowing these points and intermediate points, a smooth transition from crown to super can be constructed.

# 9.	PLANT & MATERIALS APPROVAL

Has the plant where the concrete is to be produced been approved?
(Article 1103.02)	____

Have you the Contractor notified the Engineer of his/her proposed sources of materials prior to delivery? (Article 106.05 of Tollway Supplemental Specs)	____

Has all material been inspected, tested and approved before incorporation in the work? (Article 106.03 & 106.04 of Tollway Supplemental Specs)	____

Is this project set up as Quality Control/Quality Assurance (QC/QA)?	____

If so, are you reviewing the latest version of the QC/QA documents for information regarding quality control procedures by the contractor and quality assurance by the Tollway?	____

Note:	Most PCC paving projects will be QC/QA.  The QC/QA requirements will apply to both the PCC pavement and the CAM II Stabilized subbase.  Contact Tollway Materials department for concrete testing equipment and mixture design approval.

# 10.	TEMPERATURE LIMITATIONS (Article 1020.14(a))

Is the outside air temp in the shade at least 35 °F and ascending before allowing the contractor to start mixing and placement operations?	____

Are you discontinuing your operations when a descending air temp reaches 40 °F?	____

Is the temp of the concrete between 50 °F and 90 °F at the time of placement?	____

# 11.	MIXING CONCRETE (Article 1020.11(c))

Are you the Contractor producing the concrete in conformance with one of the following methods?  Check each article for a review of requirements and restrictions for each:	____

a.	Stationary mixer. (Articles 1103.01(a) & 1020.11(a)(1))	____

b.	Truck mixed concrete. (Articles 1103.01(b) & 1020.11(a)(2))	____

# 12.	TRUCK REQUIREMENTS

Is all concrete which is mixed in a stationary mixer being deposited within 30 minutes when hauled in nonagitating trucks and within 60 minutes when hauled in agitator trucks? (Article 1020.11(a)(7))	____

Is truck mixed concrete being delivered and deposited within 60 minutes from the time stamped on the ticket? (Article 1020.11(a)(7))	____

Note:	Haul time may be increased to 90 minutes if the air temperature is between 50 ˚F and 64 ˚F or if a retarder is used.

# 13.	SEQUENCES OF FORM TYPE PAVING

Is all of the required concrete finishing equipment on the job and in acceptable working condition?  Are the following sequences for form type paving being properly followed:

a.	Placing concrete (Article 420.07).  Is the concrete being unloaded into a mechanical concrete spreader? (Article 1103.12)	____

Note:	Use of a mechanical concrete spreader may be waived if the concrete hauling equipment is equipped with a discharge system capable of distributing the concrete without segregation. (Article 1103.13)

b.	Strike-off (Article 420.09).  Is the concrete being struck off to the approximate cross section of the pavement?	____

c.	Consolidation (Article 420.09).  Is one pass of an approved surface vibrator (minimum of 3500 VPM) or internal vibrator (Article 1103.12) (minimum of 7000 VPM) being made?  Are you checking the vibrator frequency at the start of each day with a contractor furnished reed tachometer?	____

d.	Finishing (Article 420.09(a))

(1)	Is the concrete being finished by an approved finishing machine? (Article 1103.13(b))	____

or;

(2)	When breakdowns occur, hand methods will be permitted to finish up deposited concrete. (420.09(a)(2))	____

or;

(3)	When pavement width varies or is less than 10 ft in width, vibrating screed may be used for strike-off and consolidation. (Article 420.09(a)(3))	____

e.	Longitudinal floating  (Article 420.11(b))

(1)	Is the form riding mechanical float (Article 1103.15) making 
2 passes over all areas? (Article 420.09(b)(1))	____

or;

(2)	Form riding finisher float (Article 1103.14) suspended on rigid frame? (Article 420.09(b)(2))	____

or;

(3)	(In emergency or for pavements with a speed limit posted at 40 m.p.h. or less), 10 ft hand operated longitudinal float (Article 1103.17(e)). (Articles 420.09(b)(3))	____

f.	Straightedging (Article 420.09(c)) - At least two 10 ft long straight edges shall be supplied. (Article 1103.17(h))	____

g.	Edging (Article 420.09(d)) - At least two 1/4 inch radius edging tools (Article 1103.17(j)).	____

h.	Final Finish (Article 420.09(e)) – For a type A finish, is the surface of the concrete textured with a turf drag followed by a mechanically operated metal comb transverse grooving device (tining)?	____

A type B finish only requires a turf drag.

i.	Do you have available at all times a covering material such as polyethylene sheeting for the protection of the pavement in case of rain? (Article 420.07)	____

# 14.	SEQUENCES OF SLIPFORM PAVING

When you (Contractor) uses this optional method for the construction of the pavement are the following sequences being properly followed:

a.	Is the self propelled formless paver (Article 1103.16) capable of spreading, striking off, consolidating internally, and finishing the newly placed concrete in one pass to the required line and grade?
(Article 420.14)	____

b.	Are you checking the vibrator frequency at the start of each day with a contractor furnished reed tachometer? (Article 1103.12)	____

c.	Is the pavement being straightedged, edged and textured as required in the previous question? (Article 420.09)	____

d.	Do you the Contractor have available at all times metal or wooden sideforms and a covering material such as polyethylene sheeting for the protection of the pavement in case of rain? (Article 420.07)	____

e.	Are you the Contractor immediately repairing all slumping edges in excess of 1/2 inch or ¼ inch if additional concrete work is required adjacent to the pavement lane being placed? (Article 420.14(c))	____

# 15.	THICKNESS TEST

Are you checking the thickness of the pavement at least at every 250 ft location? (Before and after rod and level, before and after stringline, or direct probing measurements are all acceptable.)  Record and retain in job records.  (Articles 420.15 & 407.10)	____

# 16.	AIR CONTENT

Are you testing the concrete for air (5 - 8%) at least every 250 foot of pavement?  Record and retain in job records. (Articles 1020.08 & 1020.04 Table 1)	____

# 17.	SLUMP

Are you testing the concrete for slump (2 to 4 inches,  3/4 to 11/2 inch for slipforming) at least once each day?  Record and retain in job records.  (Articles 1020.07 & 1020.04 Table 1)	____

# 18.	STRENGTH

Are test specimens being cast at the site of work at the following frequency:	____

a.	Modulus of Rupture 6” x 6” x 30” beam

4 beams first day; 2 per day thereafter

Break @ 3, 5, 7 and 14 days.

Strength requirement = 650 psi in 14 days (Article 701.17(c)(5))

Report on, “Field Record Book of Modulus of Rupture Tests of Concrete Beams”	____

or,

b.	Compressive Strength 6” dia. x 12” cylinder.

Make 2 cylinders in lieu of each beam

Strength requirement = 3500 psi in 14 days (Article 701.17(c)(5))	____

# 19.	Sawed LONGITUDINAL JOINT  (Std. 420001)

a.	Is the longitudinal joint strengthened by 30 inch #6 tie bars at 30 inch centers at t/2 depth perpendicular to the joint?  (Article 420.05(a))	____

b.	Is the longitudinal joint being sawed to a depth of t/3 of the pavement thickness according to Article 420.05(a)?	____

# 20.	TRANSVERSE EXPANSION JOINTS

a.	Is the preformed joint filler  continuous from form to form and shaped to the subgrade or subbase? (Article 420.05(d))	____

b.	Are the smooth dowel bars positioned parallel to the grade @ t/2 depth and @ 12 inch centers?	____

c.	Are the capped ends of the bar oiled? (420.05(d)(2))

# 21.	TRANSVERSE CONTRACTION  JOINTS

a.	Are the load transfer assemblies of the size and positioning shown on Std. 420001 being pinned to the grade at the spacing shown on the Tollway Standard? (Article 420.05(c)(2), Standard 420101 or 420106)	____

b.	Is a 2 3/4 inch or t/3 deep groove being sawed over each assembly 4 to 24 hours after concrete placement? 
(Article 420.05(c)(1), Standard 420001)	____

# 22.	TRANSVERSE CONSTRUCTION JOINTS  (Article 421.04(b))

a.	Is a transverse construction joint constructed when there is an interruption of more than 30 minutes in the concreting operations?  (Article 420.05(e))	____

b.	Is the transverse construction joint located at a transverse contraction joint? (Article 420.05(e))	____

c.	Are joints formed by means of a suitable header board conforming to the cross section of the pavement and drilled for the tie bars? 
(Article 420.05(e))	____

# 23.	SURPLUS - DEFICIENCY DETERMINATION

Is a daily check being made on the yield of produced concrete?  A deficiency computation is serious; it usually indicates thin pavement.	____

DorS=Differencebetweenrequiredvolume∧volumeusedRequiredvolumex100

Where - Required volume = L’ x W’ x D’ x 1/27

Used volume = Number of batches x cy/batch

# 24.	CURING (1020.13(a))

Are the pavement surface and edges being cured for 3 days (1020.13(a)) by one of the following methods:

a.	Waterproof Paper Method. (Article 1020.13(a)(1))	____

b.	Polyethylene Sheeting Method. (Article 1020.13(a)(2))	____

c.	Wetted Burlap Method. (Article 1020.13(a)(3))	____

d.	Membrane Curing Method.  As soon as water sheen has disappeared, are 2 separate applications, separated by at least one minute, of agitated Type III (white) curing compound (Article 1022.01) being uniformly applied at a rate of One gallon/250 sf?  (Article 1020.13(a)(4))

Note:	Not allowed between November 1 & April 15 (Article 1020.13 Note 5).  Not allowed if protective coat is to be applied.  (Article 1020.13(a)(4))	____

e.	Wetted Cotton Mat Method. (Art. 1020.13(a)(5)	____

# 25.	PROTECTION

Are you the Contractor providing protection of the pavement from low temperatures as follows:  (Article 1020.13(c))

Min. Temp. Forecast 		Protection

25°F - 32° F	1 layer of poly & 1 layer burlap, or

(or if drops below 32° F	2 layers of polyethylene, or

during first 72 hours)	2 layers of waterproof paper	____

Below 25°F	6 inches of straw

covered with 1 layer of poly or

waterproof paper	____

# 26.	SURFACE VARIATIONS (420.12 & 407.09)

When the concrete has cured sufficiently to permit the testing, are you profilographing or straightedging each wheel lane for surface variations?  (Articles 420.10 & 407.09)	____

Is the required corrective work being performed? (Articles 420.10 & 407.09))	____

# 27.	OPENING TO TRAFFIC

Is the pavement being closed to traffic until:

a.	The curing and protection period has elapsed? (Article 701.17(c)(5))	____

b.	All joints have been sealed? (Article 420.12)	____

Note:	The pavement shall also be closed to construction traffic until the joints are sealed.

c.	The required strength has been achieved by test specimen?
(Article 701.17(c)(5))	____

# 28.	PROTECTIVE COAT

a.	Is a protective surface treatment being applied when pavement is constructed after October 15, and will be opened to traffic prior to the following April 15; or when directed by the Engineer? (Article 420.18)	____

b.	Are 2 coats at 50 sy/gal/coat being applied to 14 day old minimum pavement?  Is air temperature above 40 °F?
(Article 420.18)	____

# 29.	FIELD RECORDS

Are all tests, measurements, observations and computations required in the foregoing being maintained in a hard back field book?

____